## Slide 1: Characterisation and Radionuclide Transport Modelling of SNF from LWR SMRs
Sami Naumer, Miiko Pöyhönen, Veli-Matti Pulkkanen, Pirjo Hellä, Anniina Seppälä

## Slide 2: Background
Chart: Burnup and 235U enrichment of LWR SMRs fuel
| 5 | 5 | 5 | 3.1 | 4.5 | 5 | 5 | 5 | 5 | 19 | 5 | 5 | 3 | 5 | 4.5 | 4.5
burnup | 52 | 55 | 40 | 24 | 40 | 62 | 55 | 30 | 54 | 60 | 65 | 43 | 25 | 55 | 57 | 55
LWR SMRs employ similar technology as conventional nuclear power plants
SMRs fuel has similar characteristics, burnups and enrichment comparable to fuel from conventional NPPs
However, LWR SMRs have large variation in fuel enrichment and burnup [1]
How variations in burnup and enrichment affect disposal?
STAR
LDR-50
Rolls-Royce SMR
Current NPPs
Named SMRs
Other SMRs
Finnish nuclear power plants

## Slide 3: Objectives of this study
How does SNF from LWR SMRs with different burnups, and slightly varying enrichments differ? Selected reactors:
  Rolls-Royce SMR: up to 65 MWd/kgU and 4.95% 235U [1]
  LDR lite: 20–25 MWd/kgU and 2–3% 235U [2]
Characterisation of SNF for both reactors
Radionuclide transport modelling from the repository near-field using SNF inventories specified for the two SMRs
Output: Near-field release rate
for each radionuclide
SNF characterisation
Near-field model
Output: Radionuclide inventory
Fuel
Cladding
Other structural parts
To geosphere
This study

## Slide 4: SNF Characterisation
Characterisation carried out with Serpent version 2.2.2 [3]
17x17 square LWR fuel assembly in an infinite 2D lattice geometry
  Based on LDR lite, “extended” assembly for Rolls Royce (more U)
  Reflective boundary conditions
  Full power operation on three cycles
  Three different assemblies modelled for LDR lite
  One for Rolls-Royce SMR
  No impurities in materials
A) Infinite lattice geometry
B) Single assembly
C) Fuel rod in an assembly

## Slide 5: SNF Characterisation

## Slide 6: Canister loading
No new criticality calculations carried out
Assumption: similar canister as used for the fuel from EPR (OL3) [4], four assemblies in each canister for both SMRs. This canister is used as a reference canister.
  Earlier studies show that LDR lite fuel could be disposed with a fresh fuel assumption [5]
  Rolls Royce has higher discharge burnup than EPR fuel, so assumed that it also can be disposed in a similar canister. Needs to be reassessed with canister criticality calculations
LDR lite:
4 x assembly
  139 kgU
556 kgU
Rolls-Royce SMR:
4 x assembly
  389 kgU
1 557 kgU
  2.8 x to LDR lite

## Slide 7: Results
Higher burnup leads into a greater depletion of fissile materials into fission products
  Higher activity and decay heat
  For certain LDR-lite assemblies, a substantial amount of fissile material is left over
    Real operation could aim for higher burnup?
Notes: Briefly explain that three different LDR assemblies were modelled
Explain that the right-side image is normalised so that the timescale is from beginning until removal from reactor

## Slide 8: Radionuclide Transport Modelling

## Slide 9: Radionuclide transport modelling
Similar approach as applied by Posiva [6] (with newly built models)
  GoldSim software
Modelling assumptions:
  A hole appears in the reference canister after 1000 years and fuel starts to dissolve
  Stable groundwater conditions
  Diffusion through the EBS into the excavation damage zone
  Sorption and solubility limits retard release
  Advection out of the near-field
Inventory:
  Separate models for LDR lite and Rolls-Royce SMR
  Inventory divided into fuel, cladding and other structural parts
    All with separate degradation rates
Results compared to reference fuel [6]
  Note: in this study Calculated without IRF
9
Release through an advective fracture intersecting the buffer
“F route”
Release through the excavation damage zone
Release through an advective fracture intersecting the tunnel
Bentonite buffer
Tunnel backfill (bentonite)
Bedrock with fractures

## Slide 10: Release rates from the near-field
    Posiva reference fuel [6]
      Total release: 6.8 GBq
      Peak annual release 50 200 Bq/yr
      Time of peak release rate: 3 300 a
      14C largest contributor to release

## Slide 11: Release rates from the near-field
    Posiva reference fuel [6]
      Total release: 6.8 GBq
      Peak annual release 50 200 Bq/yr
      Time of peak release rate: 3 300 a
      12C largest contributor to release
    LDR lite
      Total release: 2.9 GBq
      Peak annual release 8 670 Bq/yr
      Time of peak release rate: 140 000 a
      59Ni largest contributor to release

## Slide 12: Release rates from the near-field
    Rolls-Royce SMR
      Total release: 8.9 GBq
      Peak annual release 9 880 Bq/yr
      Time of peak release rate: 350 000 a
      59Ni largest contributor to release
    LDR lite
      Total release: 2.9 GBq
      Peak annual release 8 670 Bq/yr
      Time of peak release rate: 140 000 a
      59Ni largest contributor to release

## Slide 13: What do the results mean?
14C largest in reference fuel 59Ni in SMRs
  Impurities were not included in the SMR characterisation. Activation of impurities leads into 14C formation.
  SMR metal parts contain more nickel that is activated. Also, other nuclides such as 93Mo
  Delays time of peak release!
  Other radionuclides such as 125Cs and 129I have smaller differences, mainly from burnup and mass in the reference canister
Despite lack of activated impurities, the total release from RR is the highest
  Mass in a disposal canister varies between the reactors.
     In the future, it would be useful to compare canisters with normalised loading.
  High burnup leads to a larger inventory of fission products.
  Effect of high burnup on degradation rates not considered

## Slide 14: Conclusions
A framework from reactor to repository for SMR SNF assessments was created
  Post-irradiation activities, decay heat and radionuclide inventories determined for two SMRs.
With a lower burnup, less fissile material is converted into fission products when comparing LDR lite to Rolls-Royce SMR
The radionuclide release rates differed significantly between the SMRs and the reference fuel
  Highlights importance of including impurities during characterisation. Do the vendors take this into account, especially for advanced SMRs?
  Reactor materials also affect the releases. Could the materials be optimised during design phase of SMRs to minimise activation of mobile radionuclides?
  Need for normalised canister loading or radionuclide releases per unit of energy produced!
Characterisation and canister loading was done with a lot of assumptions
  More data needed from the vendors for detailed analysis!

## Slide 15: References
International Atomic Energy Agency, “Small Modular Reactor Technology Catalogue 2024 Edition”, 2024. [Online]. Available: https://aris.iaea.org/Publications/SMR_catalogue_2024.pdf
R. Komu, R. Tuominen. "LDR lite benchmark specifications." LDR design document, LDR-PUB-VTT-10002-R4, VTT Technical Research Centre of Finland, 2024.
J. Leppänen, V. Valtavirta, A. Rintala and R. Tuominen, ”Status of the Serpent Monte Carlo code in 2024”, EPJ Nuclear Sciences & Technologies, vol 11, 2025. [Online]. Available: https://doi.org/10.1051/epjn/2024031
Posiva, “Käyttölupahakemus Käytetyn Ydinpolttoaineen Kapselointi- ja loppusijoituslaitos” 2021. [Online]. Available: https://tem.fi/documents/1410877/176068401/Kayttolupahakemus.pdf/885eff79-131c-93c3-9b36-afb5f763837c/Kayttolupahakemus.pdf?t=1697608133858
S. Naumer, P. Keto, N. Gotcheva, M. Kojo, P. Juutilainen, N. Kiviluoma, V. Rinta-Hiiro, S. Tornberg, T. Schatz, A. Vainio, M. Airola M. Lehtonen, T. Litmanen, M. Kari, ”SMRSiMa: SMR Waste Management and Siting, Waste Management and Societal Engagement”, 2024, VTT-R-00084-24
A. Poteri, H. Nordman, V-M. Pulkkanen, P. Smith, ”Radionuclide Transport in the Repository Near-Field and Far-Field”, 2014, Posiva 2014-02